## Slide 1
Recent progress in physics and technology of oxide based resistive switching memory
Yoshio Nishi
Philip Wong and Simon Wong
Electrical Engineering, Stanford SystemX Alliance
Stanford University
Stanford, California 94305-4070, USA
IEEE Silicon Valley June 8, 2015 TI Auditorium

## Slide 2: Emerging Memories
STT-MRAM
CBRAM
RRAM
PCM
Spin torque transfer magnetic random access memory
Phase change memory
Resistive switching random access memory
Conductive bridge random access memory
current
Random access, non-volatile, no erase before write

## Slide 3
On-Off Switching of RRAM
Bipolar Switching
Unipolar switching

## Slide 4: Metal Oxide RRAM (IEDM/VLSI/ISSCC)
 | NiO IEDM 2004 [1] | CuxO IEDM 2005 [2] | Cu: MoOx IEDM 2006 [3] | Ti:NiO IEDM 2007 [4] | TaOx IEDM 2008 [5] | HfOx IEDM 2008 [6] | NiO VLSI 2009 [7] | HfOx IEDM 2009 [8] | TiON IEDM 2009 [9] | Ta2O5/ TiOx VLSI 2010 [10] | WOx IEDM 2010 [11] | WOx IEDM 2010 [12] | GeO/HfON IEDM 2010 [13] | ZrOx/ HfOx IEDM 2010 [14] | N:AlOx VLSI 2011 [15] | HfOx/ AlOx VLSI 2011 [16] | TiO2/ Al2O3 VLSI 2011 [17] | TaOx/ Ta2O5 VLSI 2011 [18] | Hf/HfOx IEDM 2011 [19] | Hf/HfOx IEDM 2012 [20] | Graphene/HfOx IEDM 2012 [21] | Ni/HfOx IEDM 2012 [22] | TiON/SiO2 IEDM 2012 [23] | TaO2 O5-δ /TaOx VLSI 2012 [24] | TiOx/ Ta2O5 VLSI 2012 [25] | WO VLSI 2012 [26] | Al2O3/HfO2/Hf VLSI 2012 [27] | Nb2O5 /NbO2 VLSI 2012 [28] | TaO2 O5-δ /TaOx IEDM 2011 [29] | TaO2 O5-δ /TaOx IEDM 2012 [30] | HfOx IEDM 2012 [31] | ISSCC 2013 [32] | AlOx/WOx VLSI 2013 [33] | TaOx/ TiO2 VLSI 2013 [34] | TiO2/Al2O3 IEDM 2013 [35] | TaON IEDM 2013 [36] | TaOx/ TiO2 IEDM 2013 [37] | Ta2O5 IEDM 2013 [38] | DSA TiOx/ HfOx IEDM 2013 [39] | CuTe/ Insulator ISSCC 2014 [40]
2D/3D Geometry | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 3D Vertical | 2D Planar | 2D Planar | 3D Vertical | 3D Vertical | 3D Vertical | 3D Planar | 2D Planar | 2D Planar | 2D Planar | 2D Planar | 3D Vertical | 3D Vertical | 2D Planar | 2D Planar
SwtchTyp | Uni | Bi | Bi | Uni | Bi | Bi | Uni | Bi | Uni | Uni | Bi | Bi | Bi | Bi | Bi | Uni | Bi | Bi | Bi | Bi | Bi | Bi | Uni | Bi | Bi | Bi | Bi | Bi | Bi | Bi | Bi | N/A | Bi | Bi | Bi | Uni | Bi | Bi | Bi | Bi
Structure | 1T-1R | 1T-1R | 1R | 1T-1R | 1T-1R | 1T-1R | 1R | 1T-1R | 1T-1R | 1T-1R | 1R | 1T-1R | 1R | 1R | 1T-1R | 1R | 1T-1R | 1R | 1T-1R | 1T-1R | 1T-1R | 1T-1R | 1T-1R | 1T-1R | 1R | 1R | 1T-1R | 1S-1R | 1R | 1R | 1R | 1S-1R | 1T-1R | 1D-1R | 1R | 1R | 1R | 1R | 1R | 1S-1R
Cell Area (μm2) | ~0.2 | ~0.03 | ~25 | ~0.49 | ~0.25 | ~0.1 | 0.0023 (48nm) | 0.0009 (30nm) | 0.19 | ~3 | 8.1E-5 (9nm) | 0.0036 (60nm) | 11300 | 0.0025 (50nm) | 1 | ~6000 | 0.0029 (54nm) | ~9000 | 0.0001 (10nm) | 0.0016(40nm) | 1 | 0.0014 | 0.0308 | 0.0324 | 0.0029 | 0.001 | 0.0035 | 0.0225 | ~30nm (height) | N/A | ~4 | 0.000576 (24 nm) | 0.0324 (.18um) | 10000 | 0.0016 (40nm) | 0.0009 (30nm) | 0.2 | ~0.008 | .00011(12nm Via) | 0.004374 (27 nm)
Speed | ~5us | ~50ns | ~10ns | ~5ns | ~10ns | ~5ns | 180ns | ~300ps | ~10us | ~1us | ~1us | ~50ns | ~20ns | ~40ns | N/A | ~30ns | ~10ns | ~10ns | ~10ns | ~10ns | N/A | ~50ns | ~100us | N/A | ~10ns | ~50ns | ~10ns | ~10us | ~1us | ~1us | ~100ns | 230 us (Chip) | 100ns | 50ns | 10ns | N/A | ~1us | N/A | 100ns | 2 us (Chip)
DC Peak Voltage | <3V | <3V | <2V | <3V | <2V | <1.5V | <2V | <2.5V | <4V | <3V | <4V | <3V | <3V | <2V | <2V | <2.5V | <3V | <2.5V | <1.5V | <1.5V | <2.5V | <4.5V | <2.5V | <3V | <4V | <3V | <2V | <2V | <5V | <3.5V | <3.5V | N/A | N/A | <6.5V | <2V | <5V | <6V | <1V | <2.5V | <6.5V
DC Peak Current | ~2mA | ~45μA | ~0.5mA | ~100μA | ~17μA | ~25μA | ~90μA | ~200 μA | ~150 μA | ~200 μA | ~1μA | ~1mA | ~100nA | ~50μA | ~50nA | ~1mA | ~20μA | ~30μA | ~50 μA | ~25μA | ~200μA | ~200pA | ~60μA | ~80μA | ~50μA | ~400μA | ~500nA | ~800μA | ~80μA | ~1μA | ~50μA | N/A | N/A | ~100μA | ~1μA | ~800μA | ~0.1μA | ~100μA | ~1mA | N/A
HRS/LRS Ratio | >10 | >10 | >10 | >90 | >10 | >1,000 | >25 | >1000 | >20 | >100 | >10 | >10 | >700 | >10 | >100 | >1000 | >10 | >100 | >10 | >10 | >10 | >10 | >100 | >1000 | >10 | >10 | >10 | >10 | N/A | >20 | >10 | N/A | >10 | >105 | >100 | >100 | >10 | 8 | >10 | N/A
Endurance | 106 | 600 | 106 | 100 | 109 | 106 | 7x103 | 1010 | 106 | 105 | 200 | 106 | 106 | 106 | 105 | 106 | N/A | 1012 | 5x107 | 107 | N/A | 105 | 106 | N/A | N/A | 6x102 | 107 | 106 | 102 | 107 | 108 | N/A | 107 | 1012 | N/A | 15 | 1010 | 106 | 107 | N/A
Retention | 300h@ 150℃ | 30h@ 90℃ | 28h@ 85℃ | 1000h@ 150℃ | 3000h@ 150℃ | 10h@ 200℃ | N/A | 28h@ 150℃ | 1000h@150℃ | 120h@ 100℃ | 280h T=N/A | 2000h@150℃ | 3h@ 125℃ | 28h@125℃ | 28h@ 125℃ | 28h@ 150℃ | 100h@ 150℃ | 3h@ 200℃ | 30h@ 250℃ | 3h@ 200℃ | 27h@ 100℃ | 10yr@85℃ | 400h@ 150℃ | 100h@ 150℃ | 20@ 150℃ | N/A | 3h@250℃ | N/A | N/A | 2.8@ 85℃ | 28h@ 125℃ | N/A | 100h@85℃ | 0.27h@RT | 168h@ 125℃ | 300h@ 300℃ | 2.8h@RT | 2.8h@85℃ | 12h@ 125℃ | N/A
Compiled by PhilipWong et al )
Notes: To view then entire table, play in slideshow mode and click to advance slide. It will show the entire table. The green arrow shows you where the motion begins, and the red arrow shows where it ends.
----- 11/22/2013 re-organized by Henry
----- 12/27/2013 IEDM 2013 data added by Henry
----- 05/10/2014 ISSCC 2014 data added by Henry
[1] I. G. Baek, et al. Highly scalable nonvolatile resistive memory using simple binary oxide driven by asymmetric unipolar voltage pulses, IEDM 2004. p.587
[2] A. Chen, et al. Non-volatile resistive switching for advanced memory applications, IEDM 2005, p.746
[3] D. Lee, et al. IEDM 2006, p.1
[4] K. Tsunoda, et al. Low power and high speed switching of Ti-doped NiO ReRAM under the unipolar voltage source of less than 3 V, IEDM 2007, p.767
[5] Z. Wei, et al. Highly reliable TaOx ReRAM and direct evidence of redox reaction mechanism, IEDM 2008, p.293
[6] H. Y. Lee, et al. Ti buffer layer in robust HfO2 based RRAM, IEDM 2008, p.297
[7] B. Lee et al. NiO resistance change memory with a novel structure for 3D integration and improved confinement of conduction path, VLSI 2009, p. 28
[8] Y. S. Chen, et al. Highly Scalable Hafnium Oxide Memory with Improvements of Resistive Distribution and Read Disturb Immunity, IEDM 2009, pp. 95-98.
[9]Y. H. Tseng, et al. High Density and Ultra Small Cell Size of Contact ReRAM (CR-RAM) in 90nm CMOS Logic Technology and Circuits, IEDM 2009, pp. 99-102.
[10] Y. Sakotsubo, et al. A New Approach for Improving Operating Margin of Unipolar ReRAM using Local Minimu m of Reset Voltage. VLSI 2010.
[11] C. Ho, et al. 9nm Half-Pitch Functional Resistive Memory Cell with <1uA Programming Current Using Thermally Oxidized Sub-Stoichiometric WOx Film, IEDM 2010, pp.436-439
[12] W. C. Chien, et al. A forming-free WOx resistive memory using a novel self-aligned field enhancement feature with excellent reliability and scalability, IEDM 2010, pp. 440–443
[13] C.-H. Chang, et al. High Performance Ultra-Low Energy RRAM with Good Retention and Endurance, IEDM 2010, pp. 448-451
[14] J. Lee, et al. Diode-less nano-scale ZrOx/HfOx RRAM device with excellent switching uniformity and reliability for high-density cross-point memory applications, IEDM 2010, pp. 452–455
[15] W. Kim, et al. Forming-free nitrogen-doped AlOx RRAM with sub-uA programming current, VLSI 2011, pp. 22–23
[16] X.A. Tran, et al. High Performance Unipolar AlOy/HfOx/Ni based RRAM Compatible with Si Diodes for 3D Application, VLSI 2011, pp. 44-45
[17] J. Yi, et al. Highly Reliable and Fast Nonvolatile Hybrid Switching ReRAM Memory Using Thin Al2O3 Demonstrated at 54nm memory Array, VLSI 2011, pp. 48-49
[18] Y.-B. Kim, Bi-layered RRAM with unlimited endurance and extremely uniform switching, VLSI 2011, pp. 52–53
[19] B. Govoreanu, 10x 10 nm2 Hf/HfOx crossbar resistive RAM with excellent performance, reliability and low-energy operation, IEDM 2011, pp. 729–732.
[20] Y. Y. Chen, et al. Understanding of the Endurance Failure in Scaled HfO2-based 1T1R RRAM through Vacancy Mobility Degradation, IEDM 2012
[21] H. Y. Chen, et al. Electrode/Oxide Interface Engineering by Inserting Single-Layer Graphene: Application for HfOx–Based Resistive Random Access Memory, IEDM 2012
[22] X. P. Wang, et al. Highly Compact 1T-1R Architecture (4F2 Footprint) Involving Fully CMOS Compatible Vertical GAA Nano-Pillar Transistors and Oxide-Based RRAM Cells Exhibiting Excellent NVM Properties and Ultra-Low Power Operation, IEDM 2012
[23] W. C. Shen, et al. High-K Metal Gate Contact RRAM (CRRAM) in Pure 28nm CMOS Logic Process, IEDM 2012
[24] T. Ninomiya, et al. Conductive Filament Scaling of TaOx Bipolar ReRAM for Long Retention with Low Current Operation, VLSI, 2012
[25] H. D. Lee, et al. Integration of 4F2 Selector-less Crossbar Array 2Mb ReRAM Based on Transition Metal Oxides for High Density Memory Applications, VLSI, 2012
[26] W. C. Chien, et al. Multi-Layer Sidewall WOx Resistive Memory Suitable for 3D ReRAM, VLSI 2012
[27] L. Goux, et al. Ultralow sub-500nA operating current high-performance TiN\Al2O3\HfO2\Hf\TiN bipolar RRAM achieved through understanding-based stack-engineering, VLSI, 2012
[28] S. Kim, et al. Ultrathin (<10nm) Nb2O5/NbO2 Hybrid Memory with Both Memory and Selector Characteristics for High Density 3D Vertically Stackable RRAM Applications, VLSI 2012
[29] I. G. Baek, et al. Realization of Vertical Resistive Memory (VRRAM) using cost effective 3D Process, IEDM 2011
[30] S. G. Park, et al. A Non-Linear ReRAM Cell with sub-1μA Ultralow Operating Current for High Density Vertical Resistive Memory (VRRAM), IEDM 2012
[31] H. Y. Chen, et al. HfOx Based Vertical Resistive Random Access Memory for Cost-Effective 3D Cross-Point Architecture without Cell Selector, IEDM 2012
[32] T.-Y. Liu, et al. A 130.7mm2 2-Layer 32Gb ReRAM Memory Device in 24nm Technology, ISSCC 2013
[33] T. L. Song Reliability Significant Improvement of Resistive Switching Memory by Dynamic Self-adaptive Write Method, VLSI 2013
[34] C. -W. Hsu Self-Rectifying Bipolar TaOx/TiO2 RRAM with Superior Endurance over 1012 Cycles for 3D High-Density Storage-Class Memory, VLSI 2013
[35] B. Govoreanu, et al. Vacancy-Modulated Conductive Oxide Resistive RAM (VMCO-RRAM): An Area-Scalable Switching Current, Self-Compliant, Highly Nonlinear and Wide On/Off-Window Resistive Switching Cell, IEDM 2013
[36] M.-C. Hsieh, et al. Ultra High Density 3D Via RRAM in Pure 28nm CMOS Process, IEDM 2013
[37] C. -W. Hsu, et al. 3D Vertical TaOxTiO2 RRAM with over 103 Self-Rectifying Ratio and Sub-μA Operating Current, IEDM 2013
[38] E. Cha, et al. Nanoscale (~10nm) 3D vertical ReRAM and NbO2 threshold selector with TiN electrode, IEDM 2013
[39] Y. Wu, et al. First Demonstration of RRAM Patterned by Block Copolymer Self-Assembly, IEDM 2013
[40] R. Fackenthal, et al. A 16Gb ReRAM with 200MB/s and Write and 1GB/s Read in 27nm Technology, ISSCC 2014

## Slide 5: Energy vs Speed Trade-Off @ Device Level
https://nano.stanford.edu/stanford-memory-trends
Good corner
Nothing faster than STT-MRAM
Speed limited by physics
Notes: For RRAM and CBRAM, the energy (reset is the larger of the two energies of set and reset) for reset is mostly consumed during the time when the pulse is on and the device is still at the LRS. Therefore the longer the write time, the larger the energy and the relationship is linear (the data on the plot also has a slope of 1), and the write energy is simply a function of the resistance of the memory at LRS. Energy = power * time. So, the reset mechanism is mainly related to the power dissipation in the device irrespective of the device area (the different data points are for different device areas). For RRAM and CBRAM, to lower the energy, you want to use a large voltage pulse to get the smallest pulse width you can get away with.
For PCM, the write energy does not have a strong dependence on the write time because the write time (reset) is determined by the minimum melt quench time and the dynamic resistance of the cell (which is inversely proportional to the cell area). The various energy for the different data points are simply due to the difference device areas of the devices.
For STT-MRAM, the switching time tau is proportional to 1 / [(V_p/V_0) – 1], and the switching energy is equal to V_p^2*tau/R.
For faster switching, current larger than I_co is needed (I_co vs log t curve goes up quickly for t < 1 ns), and V_p has to increase. For larger V_p, the energy has to increase. For smaller V_p, the switching time increases, and the net result is that the switching energy decreases slightly (almost constant, depending on the switching direction) for longer write times.

## Slide 6: Write Energy Scaling @ Device Level
https://nano.stanford.edu/stanford-memory-trends
Draw a line for NAND and NOR in the energy plot
Draw a line for wire energy
Good corner
NAND
STT-MRAM Proportional to area
PCM: Proportional to area
RRAM & CBRAM: Material and resistance values
Notes: the series of data points for PCM at 180 nm node do point out that materials and device design do make a difference of about 100X. I referred to it in slide 22 (there I only say 10X because the low hanging fruits have already been picked).

## Slide 7: Memory Chip Capacity
https://nano.stanford.edu/stanford-memory-trends
64M, Unity (ISSCC)
64M, Elpida
(ISSCC)
32G, Sandisk/Toshiba
(ISSCC)
8M, Infineon
(ISSCC)
8M, Infineon,
Qualcomm,
TDK-Headway,
(VLSI)
64M, Toshiba
(ISSCC)
1G, Samsung
(ISSCC)
8G, Samsung
(ISSCC)
1G, Hynix
(VLSI)
16G,
Micron/Sony
(ISSCC)
4M, Sony
(ISSCC)
1M, Fudan
(VLSI)
128G, Samsung, Sandisk, Micron, (ISSCC)
This is the editable version
Notes: [64M, Unity (ISSCC)] Chevallier, C.J.; Chang Hua Siau; Lim, S.F.; Namala, S.R.; Matsuoka, M.; Bateman, B.L.; Rinerson, D., "A 0.13µm 64Mb multi-layered conductive metal-oxide memory," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2010 IEEE International , vol., no., pp.260,261, 7-11 Feb. 2010, doi: 10.1109/ISSCC.2010.5433945
[1M, Fudan Univ (VLSI)] Wang, M.; Luo, W.J.; Wang, Y.L.; Yang, L.M.; Zhu, W.; Zhou, P.; Yang, J. H.; Gong, X.G.; Lin, Y.Y.; Huang, R.; Song, S.; Zhou, Q. T.; Wu, H.M.; Wu, J.G.; Chi, M. H., "A novel CuxSiyO resistive memory in logic technology with excellent data retention and resistance distribution for embedded applications," VLSI Technology (VLSIT), 2010 Symposium on , vol., no., pp.89,90, 15-17 June 2010, doi: 10.1109/VLSIT.2010.5556182
[4M, ITRI (ISSCC)] Shyh-Shyuan Sheu; Meng-Fan Chang; Ku-Feng Lin; Che-Wei Wu; Yu-Sheng Chen; Pi-Feng Chiu; Chia-Chen Kuo; Yih-Shan Yang; Pei-Chia Chiang; Wen-Pin Lin; Che-He Lin; Heng-Yuan Lee; Pei-Yi Gu; Sum-Min Wang; Chen, F.T.; Keng-Li Su; Chen-Hsin Lien; Kuo-Hsing Cheng; Hsin-Tun Wu; Tzu-Kun Ku; Ming-Jer Kao; Ming-Jinn Tsai, "A 4Mb embedded SLC resistive-RAM macro with 7.2ns read-write random-access time and 160ns MLC-access capability," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2011 IEEE International , vol., no., pp.200,202, 20-24 Feb. 2011, doi: 10.1109/ISSCC.2011.5746281
[4M, Sony (ISSCC)] Otsuka, Wataru; Miyata, K.; Kitagawa, M.; Tsutsui, K.; Tsushima, T.; Yoshihara, H.; Namise, T.; Terao, Y.; Ogata, K., "A 4Mb conductive-bridge resistive memory with 2.3GB/s read-throughput and 216MB/s program-throughput," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2011 IEEE International , vol., no., pp.210,211, 20-24 Feb. 2011, doi: 10.1109/ISSCC.2011.5746286
[256k, Panasonic (IEDM)] Wei, Z.; Takagi, T.; Kanzawa, Y.; Katoh, Y.; Ninomiya, T.; Kawai, K.; Muraoka, S.; Mitani, S.; Katayama, K.; Fujii, S.; Miyanaga, R.; Kawashima, Y.; Mikawa, T.; Shimakawa, K.; Aono, K., "Demonstration of high-density ReRAM ensuring 10-year retention at 85°C based on a newly developed reliability model," Electron Devices Meeting (IEDM), 2011 IEEE International , vol., no., pp.31.4.1,31.4.4, 5-7 Dec. 2011, doi: 10.1109/IEDM.2011.6131650
[64M, Elpida] http://techon.nikkeibp.co.jp/english/NEWS_EN/20120126/203992/
[8M, Panasonic (ISSCC)] Kawahara, A.; Azuma, R.; Ikeda, Y.; Kawai, K.; Katoh, Y.; Tanabe, K.; Nakamura, T.; Sumimoto, Y.; Yamada, N.; Nakai, N.; Sakamoto, S.; Hayakawa, Y.; Tsuji, K.; Yoneda, S.; Himeno, A.; Origasa, K.; Shimakawa, K.; Takagi, T.; Mikawa, T.; Aono, K., "An 8Mb multi-layered cross-point ReRAM macro with 443MB/s write throughput," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2012 IEEE International , vol., no., pp.432,434, 19-23 Feb. 2012, doi: 10.1109/ISSCC.2012.6177078
[4M, TSMC (ISSCC)] Meng-Fan Chang; Che-Wei Wu; Chia-Cheng Kuo; Shin-Jang Shen; Ku-Feng Lin; Shu-Meng Yang; Ya-Chin King; Chorng-Jung Lin; Yu-Der Chih, "A 0.5V 4Mb logic-process compatible embedded resistive RAM (ReRAM) in 65nm CMOS using low-voltage current-mode sensing scheme with 45ns random read time," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2012 IEEE International , vol., no., pp.434,436, 19-23 Feb. 2012, doi: 10.1109/ISSCC.2012.6177079
[2M, Hynix (VLSI)] Hyung Dong Lee; Kim, S. G.; Cho, K.; Hwang, H.; Choi, H.; Lee, J.; Lee, S. H.; Lee, H. J.; Suh, J.; Chung, S.; Kim, Y. S.; Kim, K. S.; Nam, W. S.; Cheong, J. T.; Kim, J. T.; Chae, S.; Hwang, E.; Park, S. N.; Sohn, Y. S.; Lee, C. G.; Shin, H. S.; Lee, K.J.; Hong, K.; Jeong, H. G.; Rho, K. M.; Kim, Y. K.; Chung, S.; Nickel, J.; Yang, J. J.; Cho, H. S.; Perner, F.; Williams, R.S.; Lee, J. H.; Park, S.K.; Hong, S., "Integration of 4F2 selector-less crossbar array 2Mb ReRAM based on transition metal oxides for high density memory applications," VLSI Technology (VLSIT), 2012 Symposium on , vol., no., pp.151,152, 12-14 June 2012, doi: 10.1109/VLSIT.2012.6242506
[32G, Sandisk/Toshiba (ISSCC)] Tz-yi Liu; Tian Hong Yan; Scheuerlein, R.; Yingchang Chen; Lee, J.K.; Balakrishnan, G.; Yee, G.; Zhang, H.; Yap, A.; Ouyang, J.; Sasaki, T.; Addepalli, S.; Al-Shamma, A.; Chin-Yu Chen; Gupta, M.; Hilton, G.; Joshi, S.; Kathuria, A.; Lai, V.; Masiwal, D.; Matsumoto, M.; Nigam, A.; Pai, A.; Pakhale, J.; Chang Hua Siau; Xiaoxia Wu; Yin, R.; Liping Peng; Jang Yong Kang; Huynh, S.; Huijuan Wang; Nagel, N.; Tanaka, Y.; Higashitani, M.; Minvielle, T.; Gorla, C.; Tsukamoto, T.; Yamaguchi, T.; Okajima, M.; Okamura, T.; Takase, S.; Hara, T.; Inoue, H.; Fasoli, L.; Mofidi, M.; Shrivastava, R.; Quader, K., "A 130.7mm2 2-layer 32Gb ReRAM memory device in 24nm technology," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2013 IEEE International , vol., no., pp.210,211, 17-21 Feb. 2013, doi: 10.1109/ISSCC.2013.6487703
[16G, Micron/Sony (ISSCC)] Fackenthal, R.; Kitagawa, M.; Otsuka, W.; Prall, K.; Mills, D.; Tsutsui, K.; Javanifard, J.; Tedrow, K.; Tsushima, T.; Shibahara, Y.; Hush, G., "19.7 A 16Gb ReRAM with 200MB/s write and 1GB/s read in 27nm technology," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2014 IEEE International , vol., no., pp.338,339, 9-13 Feb. 2014
doi: 10.1109/ISSCC.2014.6757460

## Slide 8: Demonstrated Performance Metrics (not on the same sample) Size < 10nm X 10nm Programming Voltage < 2V Programming Current < 1mA (0.2nA) Programming Time < 10ns (0.3ns) On/Off Ratio > 103 (106) Endurance > 106 (1012) Retention > 10 years at 85OC Demonstrated Array 32Gb

## Slide 9: Performance Tradeoff In general, Programming Current ↓ , Programming Time ↑ Programming Current ↓ , On/Off Ratio ↓ Programming Current ↓ , Retention ↓ Programming Current ↓ , Endurance ?

## Slide 10: Conductive Filaments in TiO2, HfO2 and Al2O3
Ti
Vo
Al
Vo
O
Hf
Vo
O
TiO2
HfO2
Al2O3
K. Kamiya et al., PRB 2013
M. Yang et al., JJAP 2013
S. Park et al., EDL 2011
K. Kamiya et al., APL 2013

## Slide 11
Stability of Vacancies
S. G. Park, Stanford University Thesis

## Slide 12: Charge Trapping – Filament Instability
K.Kamiya, M.Y. Yang, S.G. Park, B. Magyari-Köpe, Y. Nishi, M. Niwa, and K. Shiraishi, APL 2012

## Slide 13: Atomistic Filament to Macroscopic Current Path for forming
Oxygen vacancy randomly distributed
Smaller atomistic conductive channel formations under e-field, which is one o f the two energetically stable states
Percolation path is created as atomistic channels increased
Macroscopic conductive path (percolation path) grows until tunneling starts between the tip of the conductive path and the electrode

## Slide 14
Initial (Insulator)
On (LRS)
Off (HRS)
Electro forming
Vacancies in random
Vo ordered domains
Disruption of Vo ordering
Reset
Set
Vo concentration Increases locally  Vo are ordered. (LRS)
Thermal heating by high current density  Vo diffuse out (HRS)
The resistance of each state might be determined by the amount of vacancy ordered domains. (It doesn’t have to be Magneli phase.)
Vo
Switching Modeling

## Slide 15: Challenges Scalability Uniformity / Reliability Array Architecture

## Slide 16: Recent Advances in RRAM Scaling
Potential Device Size
RRAM << NAND Flash
2D => 3D?
Z. Zhang et al., EDL 34, 2013.
B.Govoreanu et al., IEDM 2011.
K.-S. Li et al., VLSI 2014.
10 nm
X
10 nm
1 nm X 3 nm
Tip
46

## Slide 17: Sub-10 nm RRAM – Characteristics
Electrical results commensurate with typical reported RRAM
Z. Zhang, Y. Wu, H-S. P. Wong, S.S. Wong, EDL, p. 1005, Aug 2013

## Slide 18
54
DFT ab-initio modeling indicating charge localization (Off State) and charge delocalization (On state), followed by NEGF simulation
L. Zhao et al, 2014 IEDM
Notes: Here DFT calculations provide us some insights about this question. From the results, we can see that in the OFF state the wavefunctions are localized in the oxide layer. While in the ON state a delocalized conductive path is formed between the 2 electrode. This tells us that our atomic model is good for order-of-magnitude estimation of RRAM resistance.

## Slide 19: Calculated I-V Characteristics
ON state: linear I-V, Ohmic behaviors
OFF state: non-linear I-V, exponentially dependent on tOX
OFF state
ON state
55
L. Zhao et al, 2014 IEDM
Notes: Now let’s see what NEGF calculations will tell us. First we can obtain these I-V characteristics of the devices.
In ON state, we see linear I-V which implies Ohmic behaviors. This is expected because in ON state we have a metallic filament formed.
In OFF state, on the other hand, we observe nonlinear I-V characteristics. And the resistance is exponentially dependent on tox. This is also expected because the tunneling gap is the dominating factors in OFF state currents. The tunneling or hopping conduction through this gap usually has a exponential dependence on tox, to the 1st order.

## Slide 20: ON/OFF Ratio Exponentially Dependent on tOX
L. Zhao et al , 2014 IEDM
Calculated On- and Off- State Resistances and the On/Off Ratio
Notes: With these I-V characteristics we can derive the resistances and ON/OFF ratios of these devices.
Since Roff changes exponentially with tox, and Ron changes much slower in this interval, the ON/OFF ratio is also exponentially depedent on tox.
Now we have this ON/OFF ratios for our atomic model, we still needs to consider the effects of device area for real applications.

## Slide 21
2 nm- and 5 nm-HfOx Similar
2 nm
5 nm
Resistance
Distributions
60
L. Zhang etal, 2014 IEDM

## Slide 22: Challenges Scalability Reduction of Forming Voltage Uniformity / Reliability Array Architecture

## Slide 23: Bi-Layer RRAM
Y. Wu, et al., IEDM, 2013
Notes: (a) Top-view SEM picture of bi-layer TiOx/HfOx oxide RRAM device with after hole etching; (b) HRTEM image of the cross-section of the bi-layer oxide RRAM.

## Slide 24
≈10 nm RRAM Characteristics
4nm HfOX
2.5nm TiOX / 1.5nm HfOX

## Slide 25
≈10 nm RRAM Characteristics
4nm HfOX
2.5nm TiOX / 1.5nm HfOX

## Slide 26: HfO2 Partial Charge Density: Dopant + Filament
Isosurface: 0.1 e/Å3.
Undoped
Al
Si
Zr
Ni
W
Ta
L. Zhao, S. Ryu, A. Hazeghi, D. Duncan, B. Magyari-Köpe, and Y. Nishi, VLSI 2013.

## Slide 27: HfO2 Vacancy Formation Energy: Dopant + Filament
Dopant
L. Zhao, S. Ryu, A. Hazeghi, D. Duncan, B. Magyari-Köpe, and Y. Nishi, VLSI 2013.

## Slide 28: HfO2 Doping: Experiments and Theory
L. Zhao, S. Ryu, A. Hazeghi, D. Duncan, B. Magyari-Köpe, and Y. Nishi, VLSI 2013.
8.06 e20 cm-3
4.03 e20 cm-3
Undoped

## Slide 29: Al/N:AlOx/Al RRAM
Cross-section View
Ti
N-doped AlOx (RCF) / Al (BE)
Al (TE)
Al (M6)
SiO2
Al
N-doped AlOx
Al
W. Kim, et. al., Symp. VLSI Technology, p. 22 – 23, 2011
Notes: 30nm(BE)/10nm(RCM)/20nm(TE)
350 FGA for 30min, no effect on RRAM performance

## Slide 30: Al/N:AlOx/Al RRAM
125OC

## Slide 31
Seonghyun Kim et al 2012 Nanotechnology 23 325702 doi:10.1088/0957-4484/23/32/325702
Hydrogen Doping in HfO2

## Slide 32: Challenges Scalability Uniformity / Reliability Array Architecture

## Slide 33: Recent Progress – Prototype Chips
64M, Unity (ISSCC)
1M, Fudan
Univ (VLSI)
4M, Sony (ISSCC)
256k, Panasonic (IEDM)
2M, Hynix (VLSI)
4M, TSMC (ISSCC)
8M, Panasonic (ISSCC)
64M, Elpida
32G, Sandisk/Toshiba (ISSCC)
16G, Micron/Sony (ISSCC)
4M, ITRI (ISSCC)
RRAM
CBRAM
Notes: [64M, Unity (ISSCC)] Chevallier, C.J.; Chang Hua Siau; Lim, S.F.; Namala, S.R.; Matsuoka, M.; Bateman, B.L.; Rinerson, D., "A 0.13µm 64Mb multi-layered conductive metal-oxide memory," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2010 IEEE International , vol., no., pp.260,261, 7-11 Feb. 2010, doi: 10.1109/ISSCC.2010.5433945
[1M, Fudan Univ (VLSI)] Wang, M.; Luo, W.J.; Wang, Y.L.; Yang, L.M.; Zhu, W.; Zhou, P.; Yang, J. H.; Gong, X.G.; Lin, Y.Y.; Huang, R.; Song, S.; Zhou, Q. T.; Wu, H.M.; Wu, J.G.; Chi, M. H., "A novel CuxSiyO resistive memory in logic technology with excellent data retention and resistance distribution for embedded applications," VLSI Technology (VLSIT), 2010 Symposium on , vol., no., pp.89,90, 15-17 June 2010, doi: 10.1109/VLSIT.2010.5556182
[4M, ITRI (ISSCC)] Shyh-Shyuan Sheu; Meng-Fan Chang; Ku-Feng Lin; Che-Wei Wu; Yu-Sheng Chen; Pi-Feng Chiu; Chia-Chen Kuo; Yih-Shan Yang; Pei-Chia Chiang; Wen-Pin Lin; Che-He Lin; Heng-Yuan Lee; Pei-Yi Gu; Sum-Min Wang; Chen, F.T.; Keng-Li Su; Chen-Hsin Lien; Kuo-Hsing Cheng; Hsin-Tun Wu; Tzu-Kun Ku; Ming-Jer Kao; Ming-Jinn Tsai, "A 4Mb embedded SLC resistive-RAM macro with 7.2ns read-write random-access time and 160ns MLC-access capability," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2011 IEEE International , vol., no., pp.200,202, 20-24 Feb. 2011, doi: 10.1109/ISSCC.2011.5746281
[4M, Sony (ISSCC)] Otsuka, Wataru; Miyata, K.; Kitagawa, M.; Tsutsui, K.; Tsushima, T.; Yoshihara, H.; Namise, T.; Terao, Y.; Ogata, K., "A 4Mb conductive-bridge resistive memory with 2.3GB/s read-throughput and 216MB/s program-throughput," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2011 IEEE International , vol., no., pp.210,211, 20-24 Feb. 2011, doi: 10.1109/ISSCC.2011.5746286
[256k, Panasonic (IEDM)] Wei, Z.; Takagi, T.; Kanzawa, Y.; Katoh, Y.; Ninomiya, T.; Kawai, K.; Muraoka, S.; Mitani, S.; Katayama, K.; Fujii, S.; Miyanaga, R.; Kawashima, Y.; Mikawa, T.; Shimakawa, K.; Aono, K., "Demonstration of high-density ReRAM ensuring 10-year retention at 85°C based on a newly developed reliability model," Electron Devices Meeting (IEDM), 2011 IEEE International , vol., no., pp.31.4.1,31.4.4, 5-7 Dec. 2011, doi: 10.1109/IEDM.2011.6131650
[64M, Elpida] http://techon.nikkeibp.co.jp/english/NEWS_EN/20120126/203992/
[8M, Panasonic (ISSCC)] Kawahara, A.; Azuma, R.; Ikeda, Y.; Kawai, K.; Katoh, Y.; Tanabe, K.; Nakamura, T.; Sumimoto, Y.; Yamada, N.; Nakai, N.; Sakamoto, S.; Hayakawa, Y.; Tsuji, K.; Yoneda, S.; Himeno, A.; Origasa, K.; Shimakawa, K.; Takagi, T.; Mikawa, T.; Aono, K., "An 8Mb multi-layered cross-point ReRAM macro with 443MB/s write throughput," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2012 IEEE International , vol., no., pp.432,434, 19-23 Feb. 2012, doi: 10.1109/ISSCC.2012.6177078
[4M, TSMC (ISSCC)] Meng-Fan Chang; Che-Wei Wu; Chia-Cheng Kuo; Shin-Jang Shen; Ku-Feng Lin; Shu-Meng Yang; Ya-Chin King; Chorng-Jung Lin; Yu-Der Chih, "A 0.5V 4Mb logic-process compatible embedded resistive RAM (ReRAM) in 65nm CMOS using low-voltage current-mode sensing scheme with 45ns random read time," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2012 IEEE International , vol., no., pp.434,436, 19-23 Feb. 2012, doi: 10.1109/ISSCC.2012.6177079
[2M, Hynix (VLSI)] Hyung Dong Lee; Kim, S. G.; Cho, K.; Hwang, H.; Choi, H.; Lee, J.; Lee, S. H.; Lee, H. J.; Suh, J.; Chung, S.; Kim, Y. S.; Kim, K. S.; Nam, W. S.; Cheong, J. T.; Kim, J. T.; Chae, S.; Hwang, E.; Park, S. N.; Sohn, Y. S.; Lee, C. G.; Shin, H. S.; Lee, K.J.; Hong, K.; Jeong, H. G.; Rho, K. M.; Kim, Y. K.; Chung, S.; Nickel, J.; Yang, J. J.; Cho, H. S.; Perner, F.; Williams, R.S.; Lee, J. H.; Park, S.K.; Hong, S., "Integration of 4F2 selector-less crossbar array 2Mb ReRAM based on transition metal oxides for high density memory applications," VLSI Technology (VLSIT), 2012 Symposium on , vol., no., pp.151,152, 12-14 June 2012, doi: 10.1109/VLSIT.2012.6242506
[32G, Sandisk/Toshiba (ISSCC)] Tz-yi Liu; Tian Hong Yan; Scheuerlein, R.; Yingchang Chen; Lee, J.K.; Balakrishnan, G.; Yee, G.; Zhang, H.; Yap, A.; Ouyang, J.; Sasaki, T.; Addepalli, S.; Al-Shamma, A.; Chin-Yu Chen; Gupta, M.; Hilton, G.; Joshi, S.; Kathuria, A.; Lai, V.; Masiwal, D.; Matsumoto, M.; Nigam, A.; Pai, A.; Pakhale, J.; Chang Hua Siau; Xiaoxia Wu; Yin, R.; Liping Peng; Jang Yong Kang; Huynh, S.; Huijuan Wang; Nagel, N.; Tanaka, Y.; Higashitani, M.; Minvielle, T.; Gorla, C.; Tsukamoto, T.; Yamaguchi, T.; Okajima, M.; Okamura, T.; Takase, S.; Hara, T.; Inoue, H.; Fasoli, L.; Mofidi, M.; Shrivastava, R.; Quader, K., "A 130.7mm2 2-layer 32Gb ReRAM memory device in 24nm technology," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2013 IEEE International , vol., no., pp.210,211, 17-21 Feb. 2013, doi: 10.1109/ISSCC.2013.6487703
[16G, Micron/Sony (ISSCC)] Fackenthal, R.; Kitagawa, M.; Otsuka, W.; Prall, K.; Mills, D.; Tsutsui, K.; Javanifard, J.; Tedrow, K.; Tsushima, T.; Shibahara, Y.; Hush, G., "19.7 A 16Gb ReRAM with 200MB/s write and 1GB/s read in 27nm technology," Solid-State Circuits Conference Digest of Technical Papers (ISSCC), 2014 IEEE International , vol., no., pp.338,339, 9-13 Feb. 2014
doi: 10.1109/ISSCC.2014.6757460

## Slide 34: Experimental Calibration
[Jiang 2014 submitted]
Experiment & model
5 DC switching cycles
Pulse measurement & model
https://nano.stanford.edu/model.php
Notes: DC Fitting
a. Measure a large number (no less than 100) of experimental DC switching cycles from hardware. Pt/HfOx(1.69 nm)/TiOx(4.97 nm)/TiN devices are fabricated and tested for verification.
b. Sum currents at the same voltages at the same resistance states and calculate the mean I-V switching curve, shown in red curve in Fig. 2(a). We’ve compared the average I-V switching curve with the mean I-V switching curve, which shows using the mean I-V switching curve is more reasonable to reflect RRAM abrupt SET process.
c. The fitting is performed in MATLAB, where the total difference between the average switching curve data and model curve data is minimized.
Pulse Fitting
Data for pulse fitting is acquired by applying different pulse amplitudes (Fig. 3(b)) and different pulse widths with certain initial resistance values [2]. We found pulse fitting is important and necessary for the following reasons,
In a memory system, memory cells are written by a write-and-verify scheme using a series of pulses [7]. Tracking memory system performance is especially important in the case of cell disturbance, storage failure recovery, etc.
Filament evolution generally happens on a nanosecond timescale. Accessing RRAM may take less than 10ns, which requires the modeling of nanosecond RRAM device behavior.
Considering the nanosecond time scales of filament formation, DC switching fitting requires ~109 calculation per sweep with uniform time steps. At larger time steps, simulations inaccurately reflect the dynamics of the filament. As observed from experimental data in Fig. 3 (b), resistance tends to saturate after a certain elapsed time. Thus DC fitting may not capture the switching dynamics in the sub-100nsec regime.
[Jiang 2014] Jiang Z, Yu S, Wu Y, Engel J.H., Guan X and Wong H-SP, “Verilog-A Compact Model for Oxide-based Resistive Random Access Memory(RRAM)”, SISPAD (submitted), 2014
[Yu 2012] Yu S, Gao B, Fang Z, Yu H, Kang J and Wong H-SP, "A neuromorphic visual system using RRAM synaptic devices with Sub-pJ energy and tolerance to variability: Experimental characterization and large-scale modeling," Electron Devices Meeting (IEDM), vol., no., pp.10.4.1,10.4.4, 10-13, (2012)

## Slide 35: 1T1R RRAM Array
Bit Line
BL1
BL2
BLN
SL2
SLM
SL1
WL2
WLM
WL1
Word Line
Source Line
NMOS
Selection device
Control Ic
RRAM
Based on MOSIS deep-submicron lambda rule
One-Transistor-One-RRAM (1T1R)
NMOS size > 48λ2
RRAM cell size
= 36λ2
= 4F2
3λ
3λ
2λ
4λ
12λ
(F)
(F)
RRAM

## Slide 36: Challenges for Cross-Point RRAM Array
Read
Ic1
Set
VREAD
VUNSEL
or floating
Sense Amplifiers
GND
½ VSET
VSET
½ VSET
Selected cell : full VSET
Unselected cells: ≤ ½ VSET
Leaky paths also contribute to SA current
Hard to control RL by controlling Ic

## Slide 37: 3D RRAM Architectures
I. G. Baek, et al., IEDM, 2009 & 2011 (Samsung)
W.-C. Chien , et al., VLSIT, 2012 (Macronix)
L. Zhang, et al., IMW, 2013 (IMEC)
H.-Y. Chen, et al., IEDM, 2012 (Stanford/PKU)
Notes: Since 2009, several of 3D RRAM concepts have been reported including Samsung in IEDM 2011, Maronix in VLSI 2012, our group in IMDM 2012 and IMEC in IMW 2013.
All of these architecture are aimed to deliver high density NVM chips in the future.
in this talk, we will go through the details of this architecture.

## Slide 38: Technology Requirements of 3D RRAM
Notes: Non-linear selector ← no space in 3D cube
Low resistance BL pillar ← noise margin
Low resistance WL plane ← noise margin
Scalable stack height ← etch aspect ratio
On-pitch select transistor

## Slide 39: 3D Cross-Point Using Metal Planes
Vertical Transistor
Each Vertical RRAM Cell is randomly accessible in the array
H.-Y. Chen et al., IEDM, 2012
Notes: But in order to achieve cell random access, additional line selectors necessary. Please note that we still don’t need cell selector in memory array region.
For the x-y plan selection, We propose using a vertical transistor to serve as bit-line selector, whose gate is controlled by the select-line. Next, we propose to use metal plane as word line to achieve selection in the z direction. In doing so, Each Vertical RRAM Cell is randomly accessible in the array!
*Emphasize the selector-less

## Slide 40: Device Cross-Section
S. Yu, H.-Y. Chen et al., Symp. VLSI Tech. 2013

## Slide 41: 3D RRAM Switching Characteristics
Similar characteristics among the top, bottom, and control cells
Reset current: 30 µA ~ 50 µA
Notes: The data collected from 3 structures are presented. the black line with square is the data collected from the single cell in one-layer structure. The blue and red lines with triangle are the data collected from top and bottom cells in double-layer structure respectively .
The RESET current ranges from 30 to 50 uA. The three samples show similar IV characteristics.

## Slide 42: 3D RRAM Reliability Performance
Retention >105s @125oC
Endurance >108 cycles
H.-Y. Chen et al., IEDM, 2012
Notes: Reliability Performance is shown in this slide. The device can switch over 10^8 cycles. And it can maintain its state for over 10^5 seconds measured at 125 degree C.

## Slide 43: What we understood by now..
Reset process is the most energy consuming process
Reset current is almost linearly proportional to set current, i.e. smaller set compliance results in smaller reset current How much can we reduce power by vertical scaling
LRS is determined by set current compliance, and seems less dependent on device cross-sectional area under constant set compliance…filamentary nature
HRS is inversely proportional to device cross-sectional area…uniformly distributed leakage current in 2D
Charge injection and trapping determine thermodynamic stability of vacancy filament and diffusion
Bilayer structure, i.e. switching layer and vacancy sourcing layer seems promising, and oxygen/vacancy migration mechanism becomes clearer through kinetic modeling.

## Slide 44: Summary
Recent progress in understanding of resistive switching mechanisms reviewed
Scalability up to 2nm thick switching layer is demonstrated resulting in stable operation and improved forming process and endurance
A variety of cell architectures proposed, and demonstrated
Extended endurance and selector choice remain research challenges

## Slide 45
NMTRI Program Focus at Stanford
Model fundamental physics of RRAM to
- improve basic understanding including endurance failure mechanism
- explore new device concepts
Conduct experiments to
- study scalability
- reduce/eliminate forming
- improve uniformity and repeatability of switching behavior
- improve endurance and retention
Study array architectures to
- project ultimate packing density
- understand challenges in selector design
- devise innovative circuit techniques

## Slide 46: Acknowledgements Support of Industrial Sponsors of NMTRI DARPA 3D-IC Program IARPA Trusted IC Program SRC Many fellowships Contributions of many PhD students and post-doc researchers