## Slide 1: A novel microwave reflector-antenna as a resonant wireless passive mechanical sensor
Force sensing mechanism
Perturbation of the evanescent field of the resonator is caused by relative motion of a conductor.
Far field characterization
Acknowledgements
Funding: DFG GRK1322: "Micro Energy Harvesting“
T-Ceram for sample resonators.
Theodor Rinas for the force characterization rig.
References
[1] D. Kajfez et al., Dielectric resonators, Second edi. 1986
[2] G. Scholl et al., US Patent 1997,US5691698.
[3] H. Cheng et al., IEEE APSURSI, 2011, pp. 1350–1353.
[4] B. Kubina et al., IEEE SENSORS, 2013, pp. 1–4.
Motivation
Ubiquitous sensing for the internet of things.
Monitoring in harsh environments.
Chipless design gives high temperature compatibility.
Frequency shift sensing using high-Q resonator.
Integrated antenna + sensor concept.
Low complexity, low cost.
Wireless measurement scheme
Frequency shift measurement due to physical variable.
Burst signal from interrogation unit excites the resonator.
The decaying response is analyzed.
Sensor design
Maximum coupling is achieved when Qrad = Qother.
*Laboratory for Electrical Instrumentation, Department of Microsystems Engineering - IMTEK, University of Freiburg, Germany
T. Aftab *, A. Yousaf *, Thomas Ostertag**, L. Reindl *
Figure 3: Experimental determination of the maximum SNR ‘edge gap’.
2 dBi gain as an antenna.
< 1 ppm frequency tracking resolution @ 30 cm, 2.45 GHz.
Up to 5 m range with 5 dBi interrogation antenna.
**RSSI GmbH, Ulm, Germany
Antenna
Resonator
L
R
C1
CO
Reader
Dielectric resonator (TE01δ mode) in evanescent open ended waveguide.
Frequency perturbation modelled as PPDR.
Cantilever beam
Copper foil
Conductive glue
Force
Volume change
Open ended waveguide
Dielectric resonator
Bending plate approach
Figure 1: Radiation and dielectric Q matching from simulation.
Figure 2: E and H field plots of the TE01δ mode.
Figure 4: A modified waveguide with slits (left) to allow a cantilever behavior (top right). An uncut bending plate design (bottom right) .
Figure 5: Experimental sensor characterization setup(left). Force-frequency shift transfer function @ 2.46 GHz (right). Theoretical PPDR frequency perturbation action (right insert).
Figure 7: Horizontal (top) and vertical (bottom) radiation profiles.
Figure 6: Frequency measurement @ 1k samp/sec with spread probability (right).