## Slide 1: Passive Sensors and Antennas Using Stretchable Conductors
Jacob J. Adams
Department of Electrical and Computer Engineering
North Carolina State University
Antennas and Electromagnetics Lab (AEL)

## Slide 2: Outline
Antennas & Sensors Using Silver Nanowires
Ultrastretchable Wires for Reconfigurable Antennas
Textile Antennas on Nonwovens

## Slide 3: My group has collaborated to integrate new materials into RF/microwave systems over the past ten years.
3D printed materials [1], [2]
Flexible/stretchable conductors [3]
Textile antennas [4, 5]
[1] J. J. Adams et al., “Conformal printing of electrically small antennas onto three-dimensional surfaces," Advanced Materials, 2011.
[2] V. Bharambe et al., “Liquid metal-filled 3D antenna array structure with an integrated feeding network," IEEE Antennas and Wirel. Propag. Lett., 2018.
[3] L. Song et al., “Stretchable and reversibly deformable radio frequency antennas based on silver nanowires,” ACS Applied Materials & Interfaces, 2014.
[4] H. Shahariar et al., “Porous textile antenna designs for improved wearability," Smart Materials and Structures, 2018.
[5] Y. Mukai et al., “Effect of bending and padding on the electromagnetic performance of a laser-cut fabric patch antenna,” Textile Research Journal, 2019.

## Slide 4: Stretchable & deformable antenna using silver nanowires (AgNW)
0
-5
-10
-15
-20
-25
-30
L. Song et al., “Stretchable and reversibly deformable radio frequency antennas based on silver nanowires,” ACS Applied Materials & Interfaces, 2014.

## Slide 5: Wireless strain sensing using AgNW antennas
Width Strain
Length Strain
Offset-fed patch excites two modes with different resonant frequency.
Modes are sensitive to dimensional changes in orthogonal directions.

## Slide 6: Wireless strain sensing using AgNW antennas
Frequency deviation is calibrated to a linear model that accounts for cross-directional strain dependence.
Strain states up to 15% were measured and frequency response data were used to identify the state with good accuracy.

## Slide 7: Outline
Antennas & Sensors Using Silver Nanowires
Ultrastretchable Wires for Reconfigurable Antennas
Textile Antennas on Nonwovens

## Slide 8: Recent Approaches for Stretchable Conductors
[1]
[2]
[3]
[1] D. Gray, et al., “High-Conductivity Elastomeric Electronics,” Adv. Mater., vol. 16, no. 5, pp. 393–397, 2004
[2] J. Suikkola et al., “Screen-Printing Fabrication and Characterization of Stretchable Electronics,” Sci. Rep., 2016.
[3] R. Ma et al., “Knitted fabrics made from highly conductive stretchable fibers,” Nano Lett., 2014.

## Slide 9: “Ultrastretchable” Wires
S. Zhu et al., “Ultrastretchable Fibers with Metallic Conductivity Using a Liquid Metal Alloy Core,” Adv. Funct. Mater., vol. 23, no. 18, pp. 2308–2314, May 2013.
Hollow elastomeric (SEBS) fibers filled with a liquid metal (EGaIn).
Compared to stretchable conductors based on metal films or conductive particles (flakes or nanowires) in a polymer matrix, the liquid metal maintains a consistently higher conductivity over strain.
Technique lends the electrical properties of the liquid metal and the mechanical properties of the elastomer.
RF resistance scales more favorably than DC resistance due to skin effect.

## Slide 10
Lightweight, flexible and mechanically reconfigurable antennas?
At VHF and below, antennas must be physically large to support efficient long wavelength resonance.
Operators often carry or fabricate multiple antennas for different frequencies and pattern characteristics.
“Trim to tune” – antenna may only be good for one time use and extra wire, connectors, etc. must be carried.
53 lbs. field expedient antenna kit (Radio Reconnaissance Technologies, Inc)
Common Topologies
Half-wave dipole
Monopole over ground
Loop
Yagi
Vee or sloping vee

## Slide 11: Ultrastretchable dipole
Connecting the stretchable fiber to rigid RF connectors is a challenge
Wire dipole can be stretched by ~550%
Tunable from 330 MHz to 1350 MHz

## Slide 12: SEBS/EGaIn dipole has nearly identical performance to a solid copper antenna.

## Slide 13: A more directive and tunable full-wave loop can be made using the same approach.
E-plane
H-plane

## Slide 14: Growing interest in microfluidics for reconfigurable microwave electronics in recent years.
A. P. Saghati, J. S. Batra, J. Kameoka, and K. Entesari, “Miniature and reconfigurable cpw folded slot antennas employing liquid-metal capacitive loading,” IEEE T-AP, 2015.
What makes microfluidics interesting for RF electronics?
Wide range of reconfigurable states
Compatible with flexible materials
Improved linearity and power handling
M. Li and N. Behdad, “Fluidically tunable frequency selective/phase shifting surfaces for high-power microwave applications,” IEEE T-AP, 2012.
A. A. Gheethan, M. C. Jo, R. Guldiken, and G. Mumcu, “Microfluidic based Ka-band beam-scanning focal plane array,” IEEE AWPL, 2013.

## Slide 15: Thin, proximity coupled patch antenna - frequency and polarization reconfigurable
V. Bharambe et al., “Planar, multifunctional 3D printed antennas using liquid metal parasitics,” IEEE Access, 2019.

## Slide 16: Dual channels produce independent resonances at 4 and 6 GHz
16
V. Bharambe et al., “Planar, multifunctional 3D printed antennas using liquid metal parasitics,” IEEE Access, 2019.

## Slide 17: Patterns show >5 dBi gain and polarization diversity >14 dB.
V. Bharambe et al., “Planar, multifunctional 3D printed antennas using liquid metal parasitics,” IEEE Access, 2019.

## Slide 18: 2D beam steering using liquid metal parasitics
Beam steering with a single driven element.
Reduced scan loss in a scanned array.
Potential for very wideband (10:1) operation
V. Bharambe et al., “Planar 2D Beam Steering Antenna Using Liquid Metal Parasitics,” in review.

## Slide 19: H-plane tilt via a quasi-Yagi mode
DR
RD
Baseline
50 tilt
>7 dB pattern diversity

## Slide 20: E-plane tilt using four parasitic elements
RDRD
Baseline
50 tilt
>16 dB pattern diversity

## Slide 21: Outline
Antennas & Sensors Using Silver Nanowires
Ultrastretchable Wires for Reconfigurable Antennas
Textile Antennas on Nonwovens

## Slide 22: Durable, washable planar antennas on textiles
Nonwoven dielectric with polyurethane encapsulant is highly breathable and water repellent.
Screen printed conductive ink penetrates nonwoven fibers.
H. Shahariar et al., “Porous textile antenna designs for improved wearability," Smart Materials and Structures, 2018.

## Slide 23: The nonwoven-PU structure quickly wicks moisture, drying quickly.
Solid antenna
Porous antenna
For example, the porous antenna’s operating frequency shifts much less and dries more quickly than one covered by solid conductors.
Beneficial for applications where water saturation is problematic.
Material properties and response time potentially tunable for passive or active sensing.

## Slide 24
Conclusions
Several approaches for stretchable conductors and antennas were presented and applications in strain and moisture sensing were discussed.
Embedding silver nanowires or conductive flakes can produce viable microwave antennas but have limited conductivity.
Liquid metal “wires” exhibit the favorable electrical properties of the metal and favorable mechanical properties of the encasing elastomer.
These ultrastretchable wires can be fabricated for a variety of length scales to create antennas with multiple degrees of reconfigurability and superior versatility compared to electronic reconfiguration.

## Slide 25: Acknowledgments
Students
Clifford Muchler
Vivek Bharambe
Dr. Dishit Parekh
Dr. Hasan Shahariar
Lingnan Song
Dr. Amanda Mills (Myers)
Dr. Ying Liu
Dr. Ishan Joshipura
Jinwoo Ma
Dr. Yusuke Mukai
Collaborators
Dr. Michael Dickey
Dr. Yong Xu
Dr. Jesse Jur
Dr. Minyoung Suh
Southeastern Center for Electrical Engineering Education