## Slide 1: Reflection measurements at 60GHz
Date: 2018-March-05
Authors:
Name | Company | Email
Alecsander Eitan | Qualcomm | eitana@qti.qualcomm.com
Rotem Zamir | Qualcomm | rzamir@qti.qualcomm.com
Amichai Sanderovich | Qualcomm | amichais@qti.qualcomm.com

## Slide 2: Introduction
This submission presents results of lab measurements of the reflection from different materials at 60GHz band.
The goals of the measurements:
  Measuring the reflection attenuation of different materials, in different angles
  Developing a suitable model
  Produce a material based reflection coefficient data-base

## Slide 3: The Setup
2 Horn antennas, with 25dBi gain
VNA (R&S ZVA67)
2 vises
2 antenna-cable connectors
2 60G cables
2 metal stands for the antenna, covered with black absorber
2 plastic boxes (Legos)
Reflecting materials

## Slide 4: The Setup Procedures and Experiment course
Calibrating the VNA for Pt of 10[dBm], including 60G cable loss
Drawing the angles on the table
Positioning the reflecting surface with the vises
Positioning the Tx&Rx Horns in the correct angles, each at distance 34 cm from the reflecting surface
Saving the data from the VNA – S21[dB] for frequencies between 57GHz and 70GHz

## Slide 5: Setup pictures

## Slide 6: Setup pictures

## Slide 7: Setup pictures

## Slide 8: Materials
Metal – a flat metal plate used for reference
Absorber – electric wave absorber sheet
Wood – plate of solid wood
Thick carpet – carpet with thick fibers, waved on synthetic platform, used for flooring.
Wallpaper – drywall plate covered with flower patterned wallpaper, used for home decoration
Cubical wall – plate of wall from a typical cubical office – a thin fabric covering a metal plate.
Parquet – a beam of typical parquet flooring for home.
Melamine – a beam of typical melamine used for tables (Ikea style).

## Slide 9: Materials (cont)
Marble – used in home for kitchen worktop
Formica – a beam of Formica, used in house furnishing
Suspended Ceiling – typical office panel of suspended ceiling
ESD – a piece of ESD floor which can be found in labs
Drywall – a plate made of water resistant drywall
Ceramic – a ceramic tile used for flooring
Carpet – a piece of carpet used for office flooring. Short fibers, with a warp and weft pattern-like.

## Slide 10: Analysis
Free-Space Path-Loss (FSPL):
Material attenuation calculated by:

## Slide 11: Results

## Slide 12: Results

## Slide 13: Results

## Slide 14: Results
Chart: Material Attenuation as Function of Angle for Different Materials
| 10 | 15 | 20 | 22.5 | 25 | 30 | 35 | 40 | 45
Thick Carpet | 10.8395 | 9.6963 | 9.7998 | 9.7573 | 9.8472 | 14.303 | 25.176 | 13.378 | 8.6049
Wood | 12.8537 | 12.064 | 10.5051 | 9.6389 | 9.2508 | 7.2191 | 5.8823 | 5.0746 | 4.6075
Wallpaper | 13.4828 | 11.4618 | 9.8648 | 9.1766 | 9.098 | 9.229 | 10.8346 | 20.5823 | 16.3051
Cubicle Wall | 2.941 | 2.0375 | 1.1898 | 0.79661 | 0.88375 | 2.1432 | 2.9225 | 0.10732 | 1.7121
Metal | 0.3309 | 0.22642 | -0.10946 | -0.10802 | 0.21448 | 0.38378 | 0.18437 | 0.19548 | 1.6658
Melamine | 10.971 | 10.486 | 9.7758 | 9.2481 | 9.2151 | 9.6595 | 10.0093 | 9.7249 | 8.184
Marble | 7.7779 | 7.2472 | 7.3872 | 7.2541 | 6.9926 | 6.5017 | 6.2281 | 5.8105 | 5.1347
Formica | 12.0181 | 11.6187 | 11.5569 | 11.0966 | 10.7338 | 9.5787 | 8.8934 | 9.0451 | 8.539
Suspended Ceiling | 15.8897 | 14.1676 | 12.5277 | 12.438 | 12.6441 | 14.9237 | 12.5596 | 10.7808 | 11.1529
ESD | 5.6472 | 5.073 | 4.3891 | 4.0602 | 3.7872 | 3.0013 | 2.5045 | 2.0993 | 1.908
Drywall | 15.6214 | 15.9396 | 13.6497 | 11.916 | 10.8306 | 9.0138 | 8.0285 | 8.3881 | 9.9954
Ceramic | 7.8811 | 7.718 | 6.8698 | 6.5735 | 6.4486 | 5.3955 | 5.108 | 4.6732 | 4.3856

## Slide 15: Results
Chart: Material Attenuation as Function of the Angle & Vertical / Horizontal
| 20 | 30 | 40 | 45 | 50 | 60 | 70 | 80 | 90
Metal Vertical | 1.2205 | 1.5623 | 2.6435 | 2.4613 | 2.4121 | 2.5073 | 2.244 | 1.4542 | 1.8239
Metal Horizontal | 0.3309 | 0.22642 | -0.10946 | -0.10802 | 0.21448 | 0.38378 | 0.18437 | 0.19548 | 1.6658
Drywall Vertical | 19.0739 | 16.4876 | 14.5385 | 13.0382 | 12.4705 | 11.4896 | 11.5171 | 14.0023 | 18.6472
Drywall Horizontal | 15.6214 | 15.9396 | 13.6497 | 11.916 | 10.8306 | 9.0138 | 8.0285 | 8.3881 | 9.9954
Carpet Vertical | 15.7541 | 16.1293 | 15.6096 | 15.0913 | 14.8641 | 14.7824 | 15.845 | 16.059 | 18.1786
Carpet Horizontal | 25.366 | 24.7673 | 23.2971 | 22.6745 | 20.8839 | 19.4789 | 18.6017 | 17.8671 | 17.3262
Ceramic Vertical | 8.9245 | 8.5892 | 8.0112 | 7.6042 | 7.5573 | 7.6528 | 7.811 | 8.6948 | 10.6035
Ceramic Horizontal | 7.8811 | 7.718 | 6.8698 | 6.5735 | 6.4486 | 5.3955 | 5.108 | 4.6732 | 4.3856

## Slide 16: Summary
In this presentation we detailed reflection measurements results at 60GHz.
The measurements show that most tested materials reflection loss is ~0..12dB.
The reflection loss is frequency dependent.
3 materials presented resonance behavior in frequency, and 2 materials presented resonance behavior in angle.
The results show that 60GHz modem should handle frequency selective reflections.